## Slide 1: Case study 5 RF cavities: superconductivity and thin films, local defect… Group A5 M. Martinello A. Mierau J. Tan J. Perez Bermejo M. Bednarek

## Slide 2: Content
Thin Niobium film
Bulk Niobium
Modelling a step at grain boundary
Thermal and RF model

## Slide 3: Thin Niobium Film [1]
Evalutate the penetration depth using the Slater formula
F0=1.3GHz
G=270
Bulk Nb : lL = 36 nm
The difference might be explained by the large number of grains on thin Nb films = lower density of Cooper pairs ns => larger London penetration depth.
In the classical two-fluid model we have
9.5K
Df=6 kHz
From 9.5K and below, there is an increase of Cooper pairs density = the Nb film becomes superconducting
Frequency shift during cooldown. Linear representation is given in function of Y, where Y = (1-(T/TC)4)-1/2

## Slide 4
Thin Niobium film [2]
Degradation of Q0 at 1.2MV/m due to a “hot spot” : the dissipated power increases, hence lower Q. The hysteresis might be due to a irreversible degradation of the local defect.
Multipactor may explain the larger slope later.
1.2MV/m
3E9
1.5E9
H=4000 A/m for E=1.2MV/m
Rs_defect = 2mW
Vcavity = 5.36 10-3 m3 (ellipsoid)
Lcav/2=8cm
If the hot spot has been observed at 7.3cm, the surface of the defect would be the same (same H)
Another origin of the hot spot there could be multipacting.
multipactor
Hot spot
*

## Slide 5
Dissipation in Bulk Niobium
The first Q_switch is likely due to multipacting
At higher E field levels, electron emission might take place :
Some emitter sites are activated at Eapplied=2MV/m :
with a local field enhancement coefficient of 500, electric field reaches Elocal = 500 Eapplied = 1GV/m
which is enough of getting significant (dark) current (exponential Fowler-Nordheim law)
The second etching (150mm removed) was efficient (smoother surface) for removing the surface defects
After 150 µm etching
2 4 6 8 10 MV/m
1E9
1E8
1e7
After 40 µm etching

## Slide 6
Modelling a step @ grain boundary
EM model
L
H
R
L
Saturated zone
F
Non saturated zone
H0
Hmax
Hmax/H0-1
H/R
From this model we deduce the followings:
The larger the radius R, the smaller the enhancement factor: i.e. Hmax is close to Hc => larger stored energy
Defects with large lateral dimension L quenches at lower applied field => lower stored energy
At high field level, the radius of the defect has the major contribution lower the radius R => larger Pd
In the case the defect is a hole instead a bump (F<< L) then Hmax =H0 => the defect has no influence on the cavity

## Slide 7
284 mm
Modelling a step @ grain boundary
Realistic dimensions
A
B
0 H/Hc 1
0 H/Hc 1
20
Pd[W]
40
Pd[W]
1.4
1
0.6
1.6
1
0.6
1.6
1
0.6
2
1
0.5
RF only

## Slide 8
284 mm
Modelling a step @ grain boundary
Realistic dimensions
A
B
This model shows that larger grains produce more power dissipation, whatever r.
A smaller radius r leads to a higher field enhancement, as expected.
But small and large r give the same power dissipation ( in contradiction with the previous exercise)
BUT this is not in agreement with real life, where it has been shown that
larger grains seems to be less susceptible to FE.
Higher thermal conductivity at low temperatures
Higher purity ( RRR=600 )
The dissipated power does not increase dramatically with sharper edges => underestimation of the field enhancement factor
Larger grain size should lead to a better thermal dissipation through the bulk => this model shows the opposite and overestimates the maximum dissipated power.
r=1mm
r=50mm
r=1mm

## Slide 9
Thermal + RF model
Increasing Kapiza conductance
3.4
3
2
3.6
3
2
3.4
3
2
T
T
T
B0 = 0.1390 T B0 = 0.1391 T
B0 = 0.1323 T B0 = 0.1324 T
B0 = 0.1206 T B0 = 0.1207 T
B0

## Slide 10
Thermal + RF model
This model shows that the heat exchange at the cavity/He interface is better with higher Kapiza conductance:
the hot spot in the cavity is more localized
the temperature spread is larger
the quench occurs at higher B field
If k is temperature dependent, i.e k increases with T:
T5 ‘ < T5 (better thermal conduction with the bulk)
T1’ > T1 (poorer thermal conduction with the bulk)
the temperature spread is smaller.
RRR increases with increasing Nb purity, and hence the thermal conductivity
We can apply higher B field before quenching