## Slide 1: Group 6 / A
RF Test and Properties of a Superconducting Cavity
Mattia Checchin, Fabien Eozénou, Teresa Martinez de Alvaro, Szabina Mikulás, Jens Steckert
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 2
What is the necessary energy of the protons for β = 0.47?
Please give the relation between βg, λ and L. L is the distance between two neighboring cells. Calculate the value of L and Lacc (Lacc = 5L).
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 3
The CERN Accelerator School
Protons with a β of 0.47 should be accelerated.
The kinetic energy can be calculated with:
where
mc2 is the rest mass of the protons (938 MeV)  The kinetic energy of a proton at β = 0.47 is 124.7 MeV
L
Lacc
Particle Energy & Acceleration Length
For acceleration, the cavity is operated in the π-mode, hence the particle should
cross one cell in a time corresponding to half a RF period  t=1/2f
The time can be calculated with therefore
given f = 704.4MHz, the cell length is 100 mm. Lacc= 0.5m.
CASE STUDY
PRESENTATION
λ

## Slide 4
Is it necessary to know the material of the cavity in order to calculate the parameters given in the table? Please briefly explain your answer.
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 5
and are independent on the material
  → depends on e.m. field
  → depends on gap length
  → depends on potential
  → depends on gap length
depends on the inner surface
and on the volume
depends on internal energy,
accelerating length and field
The CERN Accelerator School
CASE STUDY
PRESENTATION
Geometrical Parameters

## Slide 6
The cavity is made of superconducting niobium. The operation temperature is 2 K.
Please calculate BCS component RBCS of the surface resistance according to the approximated expression
with T in K and f in MHz. Please explain qualitatively why the operational temperature of 2 K is preferable compare to operation at 4.3 K. Please explain which parameters which will modify the above approximated expression.
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 7
The CERN Accelerator School
Rbcs @ 2 K, pure niobium 5 cell tesla-type cavity:
  If:
  Where T=2 K, f= 704.4 MHz, then Rbcs = 3.21 nΩ
  Where T=4.3 K, f= 704.4 MHz, then Rbcs = 168.4 nΩ
There are several important parameters to consider:
Operational temperature of 2 K is preferable to 4.3 K:
RBCS Resistance
CASE STUDY
PRESENTATION
Δ: cooper pair condensation energy λ: London penetration depth ρ: resistivity of nc electrons
l: mean free path of nc electrons
ξ: coherence length of cooper pairs
→
indeed:


## Slide 8
If RBCS is the surface resistance, calculate the value of the quality factor (Q0) of this cavity. For real tested cavities there are more components of the surface resistance. Please give and describe these components.
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 9
residual
1,3 GHz
1MV/m
T (K)
(K-1)
2,5
1,66
If RBCS is the surface resistance, calculate Q0 of this cavity:
  Where G=161 Ω and RBCS = 3.21 nΩ @ 2K
  Then: Q0 = 5.02E10
  Description of the other components of the surface resistance for real tested cavities:
  RS = RBCS (ω, T, Δ, TC, λL , ξ0, l)+ Rres
  where the possible contributions to Rres are:
    Trapped magnetic field
    Normal conducting precipitates
    Grain boundaries
    Interface losses
The CERN Accelerator School
Unloaded Quality Factor
CASE STUDY
PRESENTATION

## Slide 10
In operation a stored energy of 65 J was measured inside the cavity. What is the corresponding accelerating gradient (Eacc)? What is the dissipated power in the cavity walls (in CW operation)?
If we take 190 mT as the critical magnetic RF surface field at 2K, what is the maximum gradient, which can be achieved in this cavity? At which surface area inside the cavity do you expect the magnetic quench (qualitatively)?
8. Verify that the calculated gradient in question 6 is lower than in question 7. Please explain qualitatively which phenomena can limit the experimental achieved gradient.
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 11
The CERN Accelerator School
CASE STUDY
PRESENTATION
r/Q: shunt impedance: 173 Ω
Lacc = 5.L
W = 65J
Eacc (meas) = 19.95 MV/m (Vs 14MV/m)
*Pdiss=ω.W/Q0
Pdiss = 5.74 Watt
Eacc(theo) = 190/5.59 = 34MV/m
Eacc(theo) > Eacc(meas)
Rs = Rbcs + Rres
Field Emission
Hmax close to equator. If Hmax > Hc2 = Quench
Rres:
Grain boundaries
Precipitates (NC)
Trapped magnetic fields, etc.
Theoretical vs. Achieved Gradient
6)
7)
8)

## Slide 12
Qexternal describes the effect of the power coupler attached to the cavity Qexternal = ω∙W/Pexternal. W is the stored energy in the cavity; Pext is the power exchanged with the coupler. In the cavity test the stored energy was 65 J, the power exchanged with coupler was 100 kW. Calculate the loaded quality factor (QL) and the frequency bandwidth () of the cavity.
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 13
The CERN Accelerator School
Loaded Quality Factor
 QL is completely dominated by Qext ! (Pext = 100kW, P0 = 5.75W)
CASE STUDY
PRESENTATION

## Slide 14
10. Please explain which technique is used to keep the frequency of the cavity on its nominal value.
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 15
Effects on cavity resonance requiring tuning:
Static detuning (mechanical perturbations)
Quasi-static detuning (He bath pressure / temperature drift)
Dynamic detuning (microphonics, Lorentz force detuning)
Tuning Mechanism
Electro-magnetic coupling
Mechanical action on the cavity
Types of Tuners
Slow tuner (mechanical, motor driven)
Fast Tuner (mechanical, PTZ or magnetostrictive)
Examples
INFN/DESY blade tuner with piezoactuators
CEBAF Renascence tuner
KEK slide jack tuner
KEK coaxial ball screw tuner
The CERN Accelerator School
Tuning / Tuners
CASE STUDY
PRESENTATION

## Slide 16
11. Assume that some normal conducting material (e.g. some piece of copper) is inside of the cavity. What are the effects on gradient and Q-value? Please explain qualitatively. How can you calculate the effects?
The CERN Accelerator School
CASE STUDY
PRESENTATION

## Slide 17
The CERN Accelerator School
Non super-conducting material in the cavity will reduce Q
If impurity located at iris  high E-field
  Heavy field emission: Decrease in Q0 at low Eacc
  → Emission of X-Rays
If located equator  high B-Field
  Rs↑ = Q0↓
  NC → heating → early loss of SC → Quench at low gradient
  Possible H enhancement if sharp edges → Quench at low gradient
How to anticipate the effetcts:
  RF + Thermal modelling
  Evaluation of field enhancement and heating
Eacc MV/m
Q0
30
1E11
NC Impurity in Cavity
CASE STUDY
PRESENTATION

## Slide 18
Thank You
The CERN Accelerator School
CASE STUDY
PRESENTATION