## Slide 1: Case Study 3c
High field large aperture magnet for a cable test facility
Goal: dipole, 100mm aperture, 15T @ 1.9K

## Slide 2: Magnetic Design
Cable | 
Aperture radius (r) | 50mm
Coil width | 60 mm
Cable width | 20 mm
Layers | 3
strands | 46
Strand diameter | 0.85 mm
Cu/Sc | 1.20
Keystone angle | 0.64 degrees
Fill factor (κ) | 0.266
Design based on Roman Arc
Conductor with is trade-off between max field and practical size
Cable can be 10-20mm, aim to minimise winding: (3*20mm =60mm)

## Slide 3
Chart: Field (T)
| 1 | 1 | 2 | 2 | 3 | 3 | 4 | 4 | 5 | 5 | 6 | 6 | 7 | 7.47 | 8 | 9 | 10 | 11 | 12 | 13 | 13.5
NbTi 1.9 K | 12359.0236 | 12359.0236 | 8798.5881 | 8798.5881 | 6914.758 | 6914.758 | 5624.9129 | 5624.9129 | 4634.4025 | 4634.4025 | 3822.8639 | 3822.8639 | 3129.9381 | 2834.8849 | 2521.2555 | 1975.4611 | 1478.411 | 1020.2678 | 593.92 | 194.0626 | 2.7608
Nb3Sn, 1.9 K | 54464.0657 | 42500.0503 | 35138.9736 | 29972.6676 | 26063.0493 | 22957.0693 | 20404.8018 | 18255.1894 | 16410.6133 | 14804.6708 | 13390.3216 | 12133.1255 | 11007.1681 | 9992.4964 | 9073.4418 | 8237.4888 | 7474.4911 | 6776.1146 | 6135.4332 | 5546.6316 | 5004.7804 | 4505.6665 | 4045.6606 | 3621.6147 | 3230.7807 | 2870.7449 | 2539.3765 | 2091.9949 | 1955.2817 | 1699.3592 | 1465.6589 | 1252.9553 | 1060.1384 | 886.1995 | 730.2187 | 591.3549 | 468.8371 | 361.956 | 270.0582
Loadline | 0 | 1458 | 1312.2
NB3Sn, 4.7 K | 47830.3819 | 37102.7061 | 30485.8611 | 25833.8411 | 22309.6587 | 19508.594 | 17207.1073 | 15269.9208 | 13609.5033 | 12166.2381 | 10897.838 | 9773.3022 | 8769.2741 | 7867.7458 | 7054.5576 | 6318.3841 | 5650.0313 | 5041.9367 | 4487.8075 | 3982.3522 | 3521.0799 | 3100.1463 | 2716.2356 | 2366.4677 | 2048.3246 | 1759.5921 | 1498.3121 | 1154.1115 | 1051.3368 | 862.6947 | 695.5642 | 548.8116 | 421.4085 | 312.4189 | 220.9884 | 146.3346 | 87.7389 | 44.54 | 16.1274

## Slide 4: Magnetic Design
 | Short Sample (ss) | Operational (op) (90% load line) | 
J0 | 388 | 349 | A.mm-2
I | 17.3 | 15.6 | KA
Bpeak | 16.0 | 14.8 | T
Outputs from Cable selection | 
Kappa (κ) | 0.266
Lambda (λ) | 1.04
Inputs | 
Aperture radius (r) | 50 mm
Coil width (w) | 60 mm
Margins |  | 
Current density (J) | 782 | A.mm-2
Field (B) | 2.10 | T
Temperature (T) | 2.80 | K

## Slide 5: Magneto-Mechanical Design
Three layer conductor coil
Shows mechanical breaks due to keystone angle
Wedges added to reduce higher harmonics.
(angles from the slides)

## Slide 6: Mechanical Design
Forces on the coil | 
Fx @ 90% Iss | 7.44 MN/m
Fy @ 90% Iss | -7.5848 MN/m
Yoke Dimensions | 
Thickness | 375mm (min)
Yoke
Coil
Stress | 
Stress on mid plane | 125MPa (acceptable)
Cylinder thickness | 35 mm (to compensate)

## Slide 7: What We learnt (Summary)
High field magnets needs wide coil & low current density
This can be expensive
Field quality is not a driver, but it is still possible to reduce high order harmonics
Iron yoke needs to be considerably large due to high field, a pre-stress can counter the stress in the coil
Stress is tricky….but we got there!!