## Slide 1
R. Cimino,
LNF INFN, Frascati, Italy & CERN, Geneva, CH.
Electron cloud Effects
and Cures.
partially founded by INFN-Gr.V nta-IMCA project.
CAS, Warsaw 6-10-2015
R. Cimino

## Slide 2: Electron cloud in accelerators
Phenomenology:
What happens to the Vacuum beam pipe in presence of the beam? (LHC Example)
Numerical model
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Mitigation strategies
Conclusion
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 3: Electron cloud in accelerators
Phenomenology:
What happens to the Vacuum beam pipe in presence of the beam? (LHC Example)
Numerical model
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Mitigation strategies
Conclusion
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 4: But: Vacuum interact with the beam!
  Beam dynamic experts design a complex and high performing machine and than somebody will design a metallic shell around it: It is a technical issue!!! with:
  Pressure better than 10 -9 mbar rapidly reached and stable
  Few pumps, no bake out (typically no space nor budget),
  Very low desorption yield
  High thermal conductivity
  High electrical conductivity
  No effect on the magnetic field!!
  Mechanically robust
  ….. And, of course, cheap!

## Slide 5: One real example to see it:
5
450 GeV – 150 ns bunch spacing: Merged vacuum @ LHC
8-10-2010

## Slide 6: Exotic Vacuum behavior @ LHC:
6
Beam 1
Beam 2
No pressure Increase
Pressure Increase
450 GeV – 150 ns bunch spacing: Merged vacuum
8-10-2010

## Slide 7: Easily solved: Installation of Solenoids

## Slide 8: Solenoids have effect on pressure!!!
Beam Intensity
Solenoid ON
A4L1
Solenoid ON
A4R1
Remove multipacting
Still primary electrons
After 20 min
DP ≈7·10-10
After 20 min
DP ≈7·10-10

## Slide 9: Solenoids have effect on pressure!!!
Beam Intensity
Solenoid ON
A4L1
Solenoid ON
A4R1
Remove multipacting
Still primary electrons
After 20 min
DP ≈7·10-10
After 20 min
DP ≈7·10-10
Evidence for:
e-Cloud
instabilities

## Slide 10: Electron-cloud history
1965 INP PSR Transverse instability & beam loss
1971 ISR e-p, 1977 Beam induced multipacting
1988 LANL PSR vertical instability &beam loss
1988 KEK PF multibunch instability
Since 1996 BEPC IHEP-KEK collaboration
1997 LHC crash program launched
1997 CESR “anomalous anti-damping” explained
1997/98 APS e- cloud study start
Since 1998 SPS e- cloud with LHC beam
2000 PS e- cloud with LHC beam
Since 1999 e- cloud at KEKB and PEP-II
Since October 2001 evidence for e- cloud at RICH
Since december 2002 e- cloud at TEVATRON
Etc etc…
G. Budker et al
K. Cornelis,
G. Arduini et al
KEK PF, 1988
M. Izawa, Y. Sato,
T. Toyomasu

## Slide 11: Vacuum in new generation accelerators is much “more” than a technical issue!
Let us see what may cause such beam and/or pressure instabilities.
The case of the:
LHC arcs

## Slide 12: Static
Cold Bore @ 1.9 K
Extreme High Static Vacuum (<< 10-13 Torr)

## Slide 13: Static
Cold Bore @ 1.9 K
Need of a Beam Screen
@ 5K< T <20K
to reduce heat load (SR, Eddy current, Impedance, etc…) on Cold bore for thermal load issues
Radial Distance
T=0, without beam

## Slide 14: Static
Cold Bore @ 1.9 K
Let us see what happens to the Beam screen Surface during operation
Radial Distance
T=0, without beam

## Slide 15: calculation
CB
BS
Radial Distance
Time = 0
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Synchrotron Radiation: Ec = 44 e V @ LHC
Ec

## Slide 16
CB
BS
Radial Distance
Time = 2 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Photon reflectivity:
SR & Surface Science
Flat Cu
Saw tooth
N. Mahne et al. App. Surf. Sci. 235, 221-226, (2004).

## Slide 17
CB
BS
Radial Distance
Time = 5 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Photoemission:(vs. hn, Q, E,T, B)
    R. Cimino, V. Baglin, I. R. Collins. Phys.Rev. ST-AB 2 63201 (1999).
Produced e- (PY): very important for single beam instabilities (K.Ohmi and F. Zimmermann PRL 2000)
SR & Surface Science

## Slide 18: Observation
SPS
Radial Distance
Time = 5 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Even in absence of SR:
e- from ionization of residual gas… etc
Beam induced multipacting is observed in SPS where no e- are photoemitted.
e-
(M.Jimenez)

## Slide 19: simulation
CB
BS
Radial Distance
Time = 10 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Beam induced el. acceleration
p +
(F.Zimmermann)
At the moment of creation
After acceleration
100
0
20
40
60
80
Energy (eV)

## Slide 20
CB
BS
Radial Distance
Time = 15 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
e- induced e- emission
Surface Science: SEY
R. Cimino et al Phys. Rev. Lett. 93, 14801 (2004).

## Slide 21
CB
BS
Radial Distance
Time = 20 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
e- induced e- emission vs. E
Surface Science
Energy Distribution Curves as function of Ep
R. Cimino et al Phys. Rev. Lett. 93, 14801 (2004).

## Slide 22: E- cloud simulation
CB
BS
Radial Distance
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
e- cloud Build-up
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Time structure vs.
Simulations.
P +
(F. Zimmermann)

## Slide 23
CB
BS
Radial Distance
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
e- induced heat load
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
Simulation
R. Cimino et al Phys. Rev. Lett. 93, 14801 (2004).
It causes Heat load!

## Slide 24
CB
BS
Radial Distance
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
p +
ph. and/or e- induced desorption
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Dynamic
pressure
increase !!!
p +
Desorbed gas
Surface Science and simulation
It is a beam/Vacuum issue!

## Slide 25: E- cloud simulation
CB
BS
Radial Distance
Time = 25 ns
+ +
+ + + +
+ + + + + +
+ + + +
+ +
P +
Beam blow up
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Time structure vs Simulations.
P +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
+ +
+ + + +
+ + + + + +
+ + + +
+ +
Jean-Luc Vay
IPAC’2012
It affects beam quality!

## Slide 26: Electron cloud in accelerators
Phenomenology:
What happens to the Vacuum beam pipe in presence of the beam? (LHC Example)
Numerical model (G. Rumolo UPAS Lectures 2015)
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Mitigation strategies
Conclusion
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 27: Numerical model of electron cloud effects
Multi-bunch beam
s
Primary and secondary electron production, chamber properties
E-cloud build up
x
y
Equations of motion of the beam particles
Noise
The build up problem
The instability problem
(see: G. Rumolo UPAS Lectures 2015)

## Slide 28: Numerical model of electron cloud effects
Coupled bunch electron cloud instability naturally needs a self-consistent solution of the electron cloud problem
  A broad time scale to cover, currently working on the problem
For the moment we simulate the two branches separately (similar to what is done for impedances):
  Electron cloud build up
    Multi-bunch
    Usually single passage, single turn or just few turns
  Electron cloud instability
    Single bunch
    Multi-turn, or even multi-kick multi-turn
Build up simulation
Instability simulation
Information on how many electrons interact with a bunch:
central density
detailed distribution
ECLOUD, PyECLOUD, POSINST, CSEC, …
HEADTAIL, PyHEADTAIL, CMAD, PEHTS, …
(see: G. Rumolo UPAS Lectures 2015)

## Slide 29: Numerical modeling: e- cloud build up
t=t+Δt
Evaluate the electric field of beam at macroparticles’ location
Generate seed e-
Move macroparticles (t  t+Δt)
Detect impacts and generate secondaries
Evaluate the e- space charge
electric field
(see: G. Rumolo UPAS Lectures 2015)

## Slide 30
t=t+Δt
Evaluate the electric field of beam at macroparticles’ location
Generate seed e-
Move macroparticles (t  t+Δt)
Detect impacts and generate secondaries
Evaluate the e- space charge
electric field
  Evaluate the number of seed e- to be generated during the current time step and generate macroparticles:
  Residual gas ionization and photoemission are implemented
  Theoretical/empirical models are used to determine macroparticle space and energy distributions
Numerical modeling: e- cloud build up

## Slide 31: Numerical modeling: e- cloud build up
t=t+Δt
Evaluate the electric field of beam at macroparticles’ location
Generate seed e-
Move macroparticles (t  t+Δt)
Detect impacts and generate secondaries
Evaluate the e- space charge
electric field
  The field map for the relevant chamber geometry and beam shape is pre-computed on a suitable rectangular grid and loaded from file in the initialization stage
  When the field at a certain location is needed a linear (4 points) interpolation algorithm is employed

## Slide 32: Numerical modeling: e- cloud build up
t=t+Δt
Evaluate the electric field of beam at macroparticles’ location
Generate seed e-
Move macroparticles (t  t+Δt)
Detect impacts and generate secondaries
Evaluate the e- space charge
electric field
  Use of PIC (Particle in Cell) algorithm for e- space charge field: Poisson equation:
with
on the boundary
  The electric field, given by:
  is calculated on the grid points and interpolated at the macroparticles’ positions

## Slide 33: Numerical modeling: e- cloud build up
t=t+Δt
Evaluate the electric field of beam at macroparticles’ location
Generate seed e-
Move macroparticles (t  t+Δt)
Detect impacts and generate secondaries
Evaluate the e- space charge
electric field
  Boris tracker is used for efficiently and accurately dealing with fast cyclotron motion and slow drift in presence of magnetic gradients
  The equation of motion is integrated to update macroparticles’ position and momentum:

## Slide 34: Numerical modeling: e- cloud build up
t=t+Δt
Evaluate the electric field of beam at macroparticles’ location
Generate seed e-
Move macroparticles (t  t+Δt)
Detect impacts and generate secondaries
Evaluate the e- space charge
electric field
  When a MP hits the wall the SEY model is employed to generate charge of emitted charge. Energy and angle also come from theoretical/experimental models.
  According to the number of emitted electrons, macroparticles can be simply rescaled or new are generated.

## Slide 35: Numerical modeling: e- cloud build up
Example: determine the bunch-by-bunch phase shift and compare it with machine measurements
(see: G. Rumolo UPAS Lectures 2015)

## Slide 36: Numerical modeling: electron cloud instability
Beam made of macroparticles is transported from one EC interaction station to the next one
Electron Cloud (EC) interaction station
At EC interaction station, beam is sliced and slices interact sequentially with electron cloud, made of macroparticles
(see: G. Rumolo UPAS Lectures 2015)

## Slide 37
The effect of the electron cloud on the beam becomes visible only after many turns
The electron cloud is re-initialized at every EC interaction station
Slicing is renewed at every turn
The mutual force between beam and electrons is computed using the same module as for the build up and kicks are applied to both
Numerical modeling: electron cloud instability

## Slide 38: Numerical modeling: electron cloud instability
Sample result, LHC  Interaction of bunch with e-cloud causes coherent instability and emittance growth, cured by chromaticity

## Slide 39: Electron cloud in accelerators
Phenomenology:
What happens to the Vacuum beam pipe in presence of the beam? (LHC Example)
Numerical model
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Mitigation strategies
Conclusion
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 40
It depend on the surface type and condition: has a big impact to simulations (see calculation for LHC).
Secondary Electron Yield (SEY)
three-step process:
 production of SEs at a depth z
 transport of the SE toward the surface
 emission of SE across the surface barrier
secondary electron emission
See: R. Cimino and T. Demma, “Electron cloud in Accelerators”
Int. Jou. of Modern Physics A Vol. 29, 1430023 (2014).
40

## Slide 41: Need of “state of the art” Surface Science systems to study SEY
Manipulator
Farady Cup
LEED + e- gun
X-ray Lamp
e- gun
Electron Analyser
Sample Prep.
Chamber for
reactions
The XPS system
41

## Slide 42: Measure of Secondary e- Yield: 2 methods
Igun - Isample
Iin
SEY= =
Iout
=
Igun
42

## Slide 43: 2nd method: Measure of Secondary e- Yield
In a µ-metal chamber
sample manipulator (also at Low T)
Sample well insulated (to measure small current Is)
A Faraday cup.
A Low energy electron gun
1mm slot
e- beam Stable between 30 - 500 eV
Currents from few nA to µA (20µC/h/mm2 - 20mC/h/mm2)
Intense spot (f < 0.5 mm) with low background
Igun - Isample
Iin
SEY= =
Iout
=
Igun
Isample
Igun
43

## Slide 44: Measure of Secondary e- Yield: 2 methods
Iout and Iin (N. Hilleret)
Advantages:
Simultaneously measure d at each energy: very fast.
Effective also for “dispersive samples” (i.e. Sponges)
Disadvantages
Gun far from the sample
(difficult to control LE e-)
Big(er) spot and no LE-SEY
Igun - Isample
Iin
SEY= =
Iout
=
Igun
ISample and Iin
Advantages:
Gun close to sample.
Reduce noise for low current measurements (i.e. insulators)
LE-SEY accessible!?!
Disadvantages
Gun need to be very stable (takes time)
More work (2 separate runs)
44

## Slide 45: Measure of Secondary e- Yield
At each Primary energy we measure Igun (with the Faraday cup) and Isample.
R. Cimino et al. Phys. Rev. Lett. 93, 14801 (2004).
Igun - Isample
SEY= 
=
Igun
Each point in d is the integral of the energy distribution of the emitted electrons
45

## Slide 46: SEY of LHC Cu @ Low energy
R. Cimino et al. Phys. Rev. Lett. 93, 14801 (2004).
Integrating the curves gives the Percentage of Secondaries and Reflected electrons
To separate “true secondaries from“re-diffused electrons is arbitrary and has not been considered in this analysis.
We observe that the contribution to of the reflected electrons at very low primary energy is, in this material, very high.

## Slide 47
Recently A. N. Andronov, A. S. Smirnov, I. D. Kaganovich, E. A. Startsev, Y. Raitses, and V. I. Demidov, (in Proceedings of ECLOUD’12 (2013), CERN-2013-002, p. 161) questioned this result based on the fact that: Long (forgotten) history of secondary electron emission studies suggests otherwise.
Theoretical
  Quantum diffraction from potential barrier
Experimental
  Difficulties of measurements at low incident electron energy
  Previous careful measurements showing contrary observation
  Probe measurements in plasma will not work

## Slide 48: While I will leave the theoretical aspects to others….

## Slide 49: Previous careful measurements showing contrary observation
Total secondary electron yield of Cu as a function of incident electron energy. 1. from the letter for fully scrubbed Cu (T=10 K). 2. Experimental data for bulk Cu after heating in vacuum (room temperature).
1. R. Cimino, et al, Phys. Rev. Lett. 93, 014801 (2004).
2. I. M Bronshtein, B. S Fraiman. Secondary Electron Emission. Moscow, Russia: Atomizdat, p. 408 (1969).
Other measurements reported the reflection coefficient of about 7% for incident electron energy below few electron volts for most pure metals.
I.H. Khan, J. P. Hobson, and R.A. Armstrong, Phys. Rev. 129, 1513 (1963).
H. Heil, Phys. Rev. 164, 887, (1967).
Z. Yakubova and N. A. Gorbatyi, Russian Physics Journal, 13 1477 (1970).
From: A. N. Andronov, A. S. Smirnov, I. D. Kaganovich, E. A. Startsev, Y. Raitses, and V. I. Demidov, (in Proceedings of ECLOUD’12 (2013), CERN-2013-002, p. 161)

## Slide 50: Previous careful measurements showing contrary observation
Total secondary electron yield of Mo as a function of incident electron energy after degassing by prolong heating of target.
I. M Bronshtein, B. S Fraiman. Secondary Electron Emission. Moscow, Russia: Atomizdat, p. 60 (1969).
Total secondary electron yield of Ge.
From: A. N. Andronov, A. S. Smirnov, I. D. Kaganovich, E. A. Startsev, Y. Raitses, and V. I. Demidov, (in Proceedings of ECLOUD’12 (2013), CERN-2013-002, p. 161)

## Slide 51: Thanks to this contribution we decided to address in details the capability of our setup to study LE-SEY.
Setting the energy scale.
Expected Setup limitations at Low energy
Study in identical conditions (same geometry etc.) atomically clean (XPS) Cu obtained by cycles of Ar+ sputtering of the “as received” Cu.
Compare it to “as received” Cu samples.
Warning: “As received” is NOT a well defined chemical state!

## Slide 52: Setting the energy scale for metals
e- Gun
Cathode
E
EF
Metallic
Sample
WG
WS
Ek
Ek + Vlenses = Eg
EF
Vacuum
field free
region
e-
Gun
At Sample
Surface
Vlenses
Vbias
DW
Ep = Eg – Vbias - DW
e-
R. Cimino et al. PR ST (2015)

## Slide 53: Expected Setup limitations @ low energy
R. Cimino et al. PR ST (2015)

## Slide 54: Clean (Ar+ Sputtered) Polycrystalline Cu
R. Cimino et al. PR ST (2015)

## Slide 55: Clean (Ar+ Sputtered) Polycrystalline Cu
R. Cimino et al. PR ST (2015)

## Slide 56: “As received” vs. Clean Cu
R. Cimino et al.
PR ST (2015)

## Slide 57: “As received” vs. Clean Cu
R. Cimino et al.
PR ST (2015)

## Slide 58: For the LHC: test HL simulations.
R. Cimino et al. PR ST (2015)

## Slide 59: For the LHC: test HL simulations.
R= d(0) = 0.8 in all cases
R. Cimino et al. PR ST (2015)

## Slide 60: For the LHC: test HL simulations.
R. Cimino et al. PR ST (2015)

## Slide 61: Electron cloud in accelerators
Phenomenology:
What happens to the Vacuum beam pipe in presence of the beam? (LHC Example)
Numerical model
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Mitigation strategies
Conclusion
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 62: Why?
Not only to study the input parameters used in simulations of multipacting and e-cloud build-ups, related instabilities
But also to simulate and prevent single bunch instabilities just connected to the mere existence of a certain density of e- in the accelerator chambers.
(K. Ohmi and F. Zimmermann PRL 2000)

## Slide 64
Optic beamline @ Bessy2
Photon energy: 20-1600 eV
a low grating (150 l/mm)
is used for 20-150 eV
a high grating (1228.1 l/mm) is used for 130-1600 eV
Samples: aluminum, copper, and stainless steal
Spot size:
0.25 mm in vertical,
1.1 mm in horizontal

## Slide 65: Reflectometer at BESSY II

## Slide 66: Samples and Sample holder
During the preliminary beam period, we measured different samples:
- as example here we show CU from LHC beam screen
The samples are isolated from the sample holder by Kapton to also measure the photo yield.
120 mm
48 mm

## Slide 67
Reflectivity from LHC Cu

## Slide 68: Roughness produce scatter light

## Slide 69: Photo Yield

## Slide 70: Electron cloud in accelerators
Phenomenology:
What happens to the Vacuum beam pipe in presence of the beam? (LHC Example)
Numerical model
The Surface Science properties of relevance:
SEY (Secondary Electron Yield);
PY (Photo Yield);
R (photon Reflectivity)
Mitigation strategies
Conclusion
R. Cimino and T. Demma
“Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023 (pag. 65).

## Slide 71
XPS
SEY
SR Reflectivity and PY (@BESSY-II)
We measure and feed material parameters (R, PY, and SEY) into simulations.
Understand their profound nature to:
Optimize chemical (mechanical) process to reduce their detrimental influence on beam.
Search for new material / coatings with intrinsically “good” parameters.
Towards mitigation Strategies….

## Slide 72
External solenoid field
Most of the existing and planned accelerator machines base the reaching of their design parameters to the capability of obtaining walls with a SEY ~1.3 or below!
Electrodes in the lattice
Surface Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Mitigation Strategies

## Slide 73
Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Electrodes in the lattice.
Efficiency
(time & final SEY)…
Stability and material choice…
Impedance. Space,
Machining costs.
If possible…
(Impedance, costs.)
External solenoid field.
Not always possible…

## Slide 74
Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Electrodes in the lattice.
Efficiency
(time & final SEY)…
Stability and material choice…
Impedance. Space,
Machining costs.
If possible…
(Impedance, costs.)
External solenoid field.
Not always possible…

## Slide 75
No field
60 Gauss solenoid field

## Slide 76
Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Electrodes in the lattice.
Efficiency
(time & final SEY)…
Stability and material choice…
Impedance. Space,
Machining costs.
If possible…
(Impedance, costs.)
External solenoid field.
Not always possible…

## Slide 77: Electrodes at DAFNE
D. Alesini et al. Phys. Rev. Lett. 110, 124801 ( 2013 )

## Slide 78: Electrodes at DAFNE
(a) Evolution of the averaged cloud density for different values of the electrode voltage. (b) e− cloud density at the end of the bunch train.
D. Alesini et al. Phys. Rev. Lett. 110, 124801 ( 2013 )

## Slide 79
Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Electrodes in the lattice.
Efficiency
(time & final SEY)…
Stability and material choice…
Impedance. Space,
Machining costs.
If possible…
(Impedance, costs.)
External solenoid field.
Not always possible…

## Slide 80
The Beam “scrubbing” effect is the ability of a surface to reduce its SEY after e- bombardment.
V. Baglin et al, LHC Project Report 472, CERN, 2001.
from LHC PR 472 (Aug. 2001):
“…Although the phenomenon of conditioning has been obtained reproducibly on many samples, the exact mechanism leading to this effect is not properly understood. This is of course not a comfortable situation as the LHC operation at nominal intensities relies on this effect…”

## Slide 81
Beam scrubbing effect with photon
See: R. Cimino et al Phys. Rew. AB-ST 2 063201 (1999)
81

## Slide 82: Study the Chemistry governing the SEY reduction (scrubbing) with X ray photoelectron spectroscopy
metal
secondary electrons
escape
depth
Atomically clean surface
“As received” surface
SEY
secondary electrons
metal
escape
depth
the effective SEY of the metal is strongly modified by the surface contamination
SEY
SEY is very Surface sensitive and XPS is a powerful tool to study its chemistry dependence

## Slide 83
electron
analyzer
X-ray photoelectron spectroscopy
KE: kinetic energy
BE: binding energy
φ: work function
KE=hv-BE-φ
FWHM = 250 meV
emiss=0°
hv=400 eV
hv=1253.6 eV
FWHM = 0.95 eV

## Slide 84
metal
binding energy (eV)
M
XPS spectroscopy of technical samples

## Slide 85
oxygen
metal
binding energy (eV)
M
M-O
XPS spectroscopy of technical samples

## Slide 86
oxygen
metal
carbon
hydrogen
M
M-O
C1s
binding energy (eV)
binding energy (eV)
C-C sp3
C-H
XPS spectroscopy of technical samples

## Slide 87
oxygen
metal
carbon
hydrogen
binding energy (eV)
binding energy (eV)
M
M-O
C1s
C-C sp3
C-H
C-C sp2
XPS spectroscopy of technical samples

## Slide 88
carbon
hydrogen
oxygen
metal
binding energy (eV)
binding energy (eV)
M
M-O
C1s
C-C sp3
C-H
C-C sp2
C-O-C
XPS spectroscopy of technical samples

## Slide 89
carbon
hydrogen
oxygen
metal
binding energy (eV)
binding energy (eV)
M
M-O
C1s
C-C sp3
C-H
C-C sp2
C-O-C
C=O
XPS spectroscopy of technical samples

## Slide 90
carbon
hydrogen
oxygen
metal
binding energy (eV)
binding energy (eV)
M
M-O
C1s
C=O
C1s
C-C sp3
C-H
C-C sp2
C-O-C
O-C=O
XPS spectroscopy of technical samples

## Slide 91
co-laminated Cu for LHC beam screen
Cu – ‘As received” technical surface
C1s
O1s
Cu3p
Cu2p
Understanding chemistry (XPS) and SEY

## Slide 92
co-laminated Cu for LHC: fully scrubbed
sp2
sp3
sp3
sp2
sp3
C-H
C-O
O-C=O
R. Cimino et al. PRL
109 064801 (2012)
SEY and XPS are directly related

## Slide 93
C-O
C
O
Cu
H
dissociation
C film growth
O2
reaction
CO2
CO
CO
Cu-O dissociation
O2
C-H dissociation
H2
sp3sp2 conversion
e- beam induced surface reactions
the contribution of all electron-induced surface reaction reduces max from 2.2 to 1.1
sp3
sp2
C
C
oxide reduction
R. Cimino et al. PRL (2012) & R. Larciprete PR ST (2013)

## Slide 94
The chemical origin of the scrubbing is now clear: it is due to Electron induced surface graphitization!
It occurs (with small differences) for many technical surface like Cu, SS, TiN etc. (noticeably not for Al)
BUT: it is a phenomenon which intrinsically need energy to occur: do all electrons induce it?

## Slide 96
co-laminated Cu for LHC beam screen
R. Cimino et al. PRL 109 064801 (2012)

## Slide 97
co-laminated Cu for LHC beam screen
sp2
sp3
sp3
sp2
sp3
C-H
C-O
O-C=O
R. Cimino et al. PRL
109 064801 (2012)
sp2

## Slide 98
R. Cimino et al. PRL 109 064801 (2012)
optimize the “scrubbing” process @ LHC with beam parameters enhancing the presence, in the cloud, of higher energy el.
Give a more reliable estimate of the needed scrubbing time.

## Slide 99
Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Electrodes in the lattice.
Efficiency
(time & final SEY)…
Stability and material choice…
Impedance. Space,
Machining costs.
If possible…
(Impedance, costs.)
External solenoid field.
Not always possible…

## Slide 100
C film thickness 2-3 nm
a-C films
magnetron sputtering @ RT
p(Ar)= 10-2 mbar t = 2min
R. Larciprete et al, App. Surf. Science 2015
C films on polycristalline Cu

## Slide 101
C films on polycristalline Cu
R. Larciprete et al, App. Surf. Science 2015

## Slide 102
C films on polycristalline Cu
2p-
2p-
the graphitization of the C films corresponds to a lower SEY
R. Larciprete et al, App. Surf. Science 2015

## Slide 103
at LT: Kuzucan, et al JVSTA 30, 051401 (2012)
a-C bases its stability on its low reactivity
If, on any surface, condensed gas is chemi or physi-sorbed the resulting SEY will be the one of the contaminant layer.
Kuzucan, et al JVSTA 30, 051401 (2012)

## Slide 104
If annealing (@ ~ 200 °C) is possible: TiZrV
Activated NEG: it pumps, low SEY, stable: ideal mitigator
Kuzucan, et al JVSTA 30, 051401 (2012)
Scheuerlein et al. Appl. Surf. Sci. 172 (2001) 95-102

## Slide 105
Scrubbing
(or conditioning)
Intrinsically low
SEY material
Geometrical modifications
Electrodes in the lattice.
Efficiency
(time & final SEY)…
Stability and material choice…
Impedance. Space,
Machining costs.
If possible…
(Impedance, costs.)
External solenoid field.
Not always possible…

## Slide 106: Geometrical Mitigation:
dmax,< .8 …
Impedence?

## Slide 107: Impedance enhancement factor
(Code : Finite Element Method, PAC07 THPAS067, L Wang)
The total impedance enhancement=  * percentage of grooved surface
p=1.25mm (period)
d=2.5mm (depth)
t=0.125mm (thickness)
p=1.25mm
d=2.5mm
t=0.25mm

## Slide 108: Sponge materials: R. Cimino, A. Romano, S. Petracca, I. Masullo, M. Taborelli etc: (IPAC 2014)

## Slide 109: Sponge materials: R. Cimino, A. Romano,S. Petracca, I. Masullo, M. Taborelli etc: IPAC 2014)

## Slide 110: Sponge materials: R. Cimino, A. Romano,S. Petracca, I. Masullo, M. Taborelli etc. (IPAC 2014)

## Slide 111: Sponge materials: R. Cimino, A. Romano,S. Petracca, I. Masullo, M. Taborelli etc. (IPAC 2014)
Impedance, vacuum behaviour, desorption properties
are still under study
but seems very promising.

## Slide 112
Not only low SEY, PY and R

## Slide 113: Conclusion
Electron-Cloud is and will be an important issue in circular accelerators in years to come!
Numerical simulations are able to predict observed effects.
Mitigation techniques are developing.
Synergic efforts, dedicated Surface, Material and Vacuum science laboratories are required to reach desired performances.

## Slide 114: Acknowledgements
Davide Remo Grosso, INFN-LNF, Frascati (RM), Italy
Mario Commisso, INFN-LNF, Frascati (RM), Italy
Dafne-L and Dafne Accelerator group.
Roberto Flammini, CNR-IMIP, Montelibretti (RM), Italy
Reiner Wanzenberg, Desy, Hamburg, Germany
V. Baglin, M. Jimenes, M. Taborelli, P, Chiggiato, G. Rumolo, G. Iadarola, etc… CERN, Geneva, Switzerland
Wolfram Fischer, Brookhaven Nat. Lab., USA
Rosanna Larciprete and Antonio Di Trolio,
CNR-ISC, Roma, Italy
Franz Schäfers Institute for Nanometre Optics
and Technology (INT) Berlin

## Slide 115: Acknowledgements
Davide Remo Grosso, INFN-LNF, Frascati (RM), Italy
Mario Commisso, INFN-LNF, Frascati (RM), Italy
Dafne-L and Dafne Accelerator group.
Roberto Flammini, CNR-IMIP, Montelibretti (RM), Italy
Reiner Wanzenberg, Desy, Hamburg, Germany
V. Baglin, M. Jimenes, M. Taborelli, P, Chiggiato, G. Rumolo, G. Iadarola, etc… CERN, Geneva, Switzerland
Wolfram Fischer, Brookhaven Nat. Lab., USA
Rosanna Larciprete and Antonio Di Trolio,
CNR-ISC, Roma, Italy
Franz Schäfers Institute for Nanometre Optics
and Technology (INT) Berlin